[image: image1.png]\w"
ChMmENLKTHERAF

HANGZHOU HAILAN CHEMICAL CO.,LTD



  CERTIFICATE OF ANALYSIS                                             

                                                           COA No.:HL202453
	Product Name
	Bisphenol AF

	CAS Registry number
	1478-61-1

	Structure 
	[image: image2.png]




	MF & MW
	C15H10F6O2& 336.23

	Batch number 
	202501131

	Date of manufacture 
	20250113


	Index Name
	Specifications 
	Results 

	Appearance  
	White powder
	White powder 

	Purity 
	99.5%min 
	99.5%

	Water 
	0.10% Max.
	0.06%

	Melting point 
	159.0-163.0℃
	Pass 

	Conclusion
	Up to in-house standard 


