[image: image1.png]\w"
ChMmENLKTHERAF

HANGZHOU HAILAN CHEMICAL CO.,LTD



  CERTIFICATE OF ANALYSIS                                             

                                                          COA No.:HL08202565
	Product Name
	Strontium phosphate

	CAS Registry number
	14414-90-5

	MF 
	Sr3(PO4)2

	Batch number 
	20250225

	Date of manufacture 
	20250225


	Index Name
	Specifications 
	Results 

	Characters 
	White powder
	conform

	Assay(Sr3(PO4)2)
	99.0%min 
	99.1%

	Fe
	0.1%max 
	0.005%

	As 
	0.1%max 
	0.07%

	Pb 
	0.001%max 
	Pass 

	Water 
	0.2%max 
	0.1%



	Particle size 
	99%min pass 100mesh 
	99.6%

	Conclusion 
	Up to the standard 


